## Slide 1: An Innovative Method for Mitigating Impacts from Acid-Producing Rock
By Jim Gusek, P.E. Golder Associates Inc.
Brian Masloff & John Fodor, Cellular Concrete Solutions LLC

## Slide 2: Acid Rock Drainage

## Slide 3: Overview of Best Practice Methods
Sources
Pathways
Receptors
Groundwater Perspective
Measure
Performance
Vertical Pathway
Intervention
REF: GARD Guide 2010
www.gardguide.com
Early avoidance of ARD problems is a best practice technique that is integrated into mine planning, design and waste mgt strategies

## Slide 4: Acid Rock Drainage Tetrahedron
Oxidizer
(Air, Fe+3)
Bacteria
Pyrite
Water
Fuel
Air
Heat
FIRE
ARD

## Slide 5: ARD Mitigation Framework
REF:
GARD Guide
2010
Also see:
Coal Mine Drainage Prediction and Pollution Prevention in Pennsylvania; Brady et al., 1998
Planning for avoidance
Passivation
Co-disposal, in-pit disposal… bactericides, alkaline materials, organics

## Slide 6: Best Practice Methods (1)
Avoidance
Special handling methods
  Incorporate into mine plan
  Segregation
  Tailings desulphurization
  Compaction and conditioning
  Encapsulation and layering
  Blending
  Co-disposal
  Permafrost and Freezing
Best Practice Methods - Avoidance
REF: GARD Guide 2010
What about abandoned mines?
Re-mining; backfilling; passivation; hydrodynamic controls

## Slide 7: Best Practice Methods
Dry Cover Methods
  Soil
  Alkaline
  Organics
  $ynthetics
  Gas barriers
  Vegetation
  Landform design
Water Cover Methods
  Subaqueous disposal
  Partial water cover
  Wetland covers
  Attenuation
  Stream flow regulation
  Water recycle and reuse
Best Practice Methods (Decommissioning)
REF: GARD Guide 2010
Re-mining; backfilling; passivation; hydrodynamic controls

## Slide 8: Best Practice Methods (2)
Additions and Amendment Methods
  Passivation
  Alkaline materials
  Organics
  Bactericides (Brady, Ch. 15)
Water Management Methods
  Hydrogeological & Hydrodynamic Controls
  Dewatering
  Diversion
  Flooding
  Seals
Best Practice Methods- Passivation
???
How do you to implement these methods at abandoned mines?
Re-mining; backfilling; passivation; hydrodynamic controls

## Slide 9: THE REAL PROBLEM: A Medical Analogue
ARD is a global bacterial infection.
There are plenty of geo-antibiotics available but the current situation is akin to the patient taking a shower with Tums dissolved in orange juice - not very effective or practical.
What’s needed is a mining-analogue to an I-V drip of tetracycline and/or oral antibiotics.
And then there’s the question: Do we need to Vaccinate or Medicate?
What is currently available in the ARD prevention “pHarmacy”?

## Slide 10: Known bactericides
Sodium lauryl sulfate (EPA-endorsed)
Alkyl-benzene sulfonate (laundry soap)
Waste milk (bacteria out-complete acido-thiobacillus)
Sodium Thiocyanate (NaSCN)
Bi-Polar Lipids
Note: We need to consider the physics of delivering and distributing a weak bactericide solution into a porous, unsaturated medium (it’s been done, but it wasn’t easy)

## Slide 11: Cheap alkalinity (acidity)
Limestone (quarried) – crusher fines?
Dolomite
Lime kiln dust or cement kiln dust
Steel slag
Sodium bicarbonate
Note: We need to consider the physics of delivering and distributing a solid into a porous unsaturated medium

## Slide 12: Cheap organics (oxygen)
Sawdust (the finer, the better)
Paper (newsprint, office waste [shredded])
De-inking residue
Biosolids
MicroCgTM, LactoilTM, others?
Note: We need to consider the physics of delivering and distributing a solid into a porous, unsaturated medium

## Slide 13: Passivation coatings (oxygen)
Keeco Mix (micro-silica)
Potassium permanganate (Glen Miller, UNR)
Oil and latex based paint
Potassium humate (commercial agricultural amendment)
Others?
Note: We need to consider the physics of delivering and distributing a coating into an unsaturated porous medium

## Slide 14: One Particular Problem
Deliver bactericides without complete flooding of waste rock mass
Focus the delivery of alkalinity in the “hot zones”
Deliver organics in hot zones and without complete flooding
Treating existing waste rock dumps

## Slide 15: Has it been done before?
Fisher Coal Mine, PA – 1995 Vapco Engineering
  Geophysics targets 3 ARD–generating zones
  Multiple injection boreholes on a tight spacing
  Injection of 20% NaOH solution simultaneously into 12 shallow (3 m deep) boreholes with packers
  Injection of 2% sodium lauryl sulfate bactericide
  Seepage continues to be net alkaline 16 years later, bond release is reportedly imminent

## Slide 16: Has it been done before?
Sesquatchie Coal Mine, TN – 2008 Western Research Institute
  Geophysics used to target ARD
  Two doses - drip application of waste milk and biosolids (as inoculant)
  Seepage reportedly net alkaline after four years.
  Patent issued January, 2012
  Check out ITRC website
THERE HAS TO BE A BETTER WAY
http://www.itrcweb.org/miningwaste-guidance/cs31_sequatchie.htm
Ref: Jin et al., 2007

## Slide 17: Perhaps a better way:
Use waste milk (biocide) in the liquid phase
Use sodium lauryl sulfate (bactericide) as part of the surfactant mix
Add powdered limestone for alkalinity
Add paper, sawdust, or biosolids as the organic (hoof & horn protein surfactant too)
Use engineered FOAM as a delivery medium for bactericide “cocktail”

## Slide 18: Perhaps a better way:
Use engineered FOAM as a delivery medium for bactericide “cocktail”
This process is very similar to pressurized grouting, only the grout mass is mostly gaseous, engineered to be temporary, and designed to deposit a coating of active ingredients

## Slide 19: Foam Characteristics (Think shaving cream – a LOT of it)
Two-phase “colloid”, the gas phase is separated by a liquid phase
Foam can contain a third phase – suspended solids
“Dry” foam (e.g., shaving cream)
“Wet” foam (e.g., hand soap)

## Slide 20: Adding pHoamTM containing powdered limestone to gravel in the lab

## Slide 21: Recent Experiments in the Laboratory
Limestone-Coated Gravel

## Slide 22: Recent Experiments in the Laboratory
Garden hose tremmie pipe

## Slide 23: What’s the difference between foam and pHoamTM ???
pHoamTM is a mixture of traditional foam plus one or more “active ingredients” that induce a desirable biological, geochemical, or process-related reaction
or
Foam + active ingredients that suppress an undesirable reaction.

## Slide 24: Some Potential Application Concepts
Vaccination (Prevention) | Medication (Mitigation)
Waste rock dumps at active mines (“sterilize” ARD rock by the truckload before it is placed in the dump) | Small-scale “dog hole” abandoned underground mines that produce ARD
Active coarse coal refuse piles (sterilize refuse by adding a “wet” pHoamTM in the feed hopper of a conveyor belt) | Waste rock dumps or coarse coal refuse facilities at abandoned mines (even if they are capped)
Active tailings storage facilities (sterilize the cycloned coarse tails in the embankment – the material most likely to form ARD before capping and revegetation) | Abandoned underground mine stopes (use geophysics for targeting and inject pHoamTM through bore holes) – use mine fire/foam equipment?
Active underground mine stope backfill materials | Backfilled pits (coal or metal) that are poorly capped

## Slide 25: Application Concept: Mine Dumps
Waste Rock Dump = Big Humidity Cell

## Slide 26: Application Concept: Mine Dumps
Waste Rock Dump

## Slide 27: pHoam injection kinetics - theory
Chart: Theoretical pHoam front velocity, ft/min vs. circular bulb radius, ft
| 2.5 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25 | 27.5 | 30
pHoam front velocity, ft/min | 0.88496 | 0.22124 | 0.098329 | 0.05531 | 0.035399 | 0.024582 | 0.018061 | 0.013828 | 0.010925 | 0.0088496 | 0.0073138 | 0.0061456
Elapsed time, minutes | 0.047083 | 0.37666 | 1.2712 | 3.0133 | 5.8854 | 10.1699 | 16.1494 | 24.1064 | 34.3234 | 47.0829 | 62.6673 | 81.3592
Assumed injection conditions: 29% voids, pHoam injected at 3.7 cy/min (100 cfm)

## Slide 28: Application Concept: Mine Dumps
Injection Borehole
After G.W. Wilson, 2008

## Slide 29: The “Heat-Seeking Missile” Effect in ARD Suppression
Pyrite oxidation is exothermic
If a pHoamTM encounters a “hot zone” with elevated pyrite, the bubbles should collapse and preferentially deposit the “active ingredients”
This feature could potentially give pHoamTM a “heat-seeking missile” capability that could automatically deliver more ARD-suppressing active ingredients to a mine waste site in the zones where it is needed the most.

## Slide 30: Implementation Concepts
pHoam injection system layout is simple

## Slide 31: Teaming Partners
Golder Associates Inc.
  Water Treatment and Geochemistry Groups
  Colorado School of Mines Chemistry Dept.
  Golder Construction Division
Cellular Concrete Solutions LLC (CCS)
Site owner/operator or interested entities like watershed groups

## Slide 32: Development Steps
Initial patent filing (16 August 2011)
Initial demo – injecting into a gravel-filled pipe (done)
Lab Testing (4Q 2011 to 2Q 2012)
  Entity provides pyrite waste rock dump samples (done)
  CCS treats samples with foam & amendments (done)
  Golder/CCS conducts humidity cell tests in-house (ongoing)
  CCS evaluates foam flow through porous medium (gravel) [planned]
Demonstration Site (injecting into a real dump) 3Q 2012
Monitor demo site Q4 2012 and beyond

## Slide 33: What about CO$T$????
Need to do comparison with perpetual ARD treatment (either active or passive technologies) or other remedies
We have a cost model but it has not been validated/ calibrated, so we need demonstration sites
Example: to perpetually treat ARD from a 73 hectare waste rock dump in Western USA would cost about $US 30 million. If one assumes that only 25% of the total dump volume would accept or require pHoamTM, the treatment cost is on the order of $US 15 million.
Longevity of the treatment is a big issue. The non-pHoamTM treatment at the Fisher Coal Mine in 1995 with NaOH and bactericide is still effective after 16 years.

## Slide 34: What about CO$T$????
Our cost model is appears to be most sensitive to the cost of solid active ingredients and the surfactant.
Even a minor credit for disposal of a local waste (e.g., biosolids) could result in a break-even condition.
Without the credit, cost of treatment might be less than $1.00 per ton of rock to a fraction of that, depending on whether the rock is “vaccinated” or “medicated”.

## Slide 35: Ideal pHoamTM Demonstration Site
Has re$earch funding available
Contains mine waste that is fully characterized, mapped, and is acid-generating
Is relatively small in scale (1 to 2 acres) (<1Ha)
Is relatively accessible by conventional construction equipment
Is amenable to “dissection” after pHoam application
Has documented ARD impact
Is on publicly-owned land (USFS, USBLM, USEPA Superfund)
Is not a part of or contingent upon ongoing litigation

## Slide 36: WHY IS pHOAMTM SO SPECIAL?
Uses very little water
Flexible design (wet/dry/stiff/flow-able)
Flexible longevity (hours to days)
Flexible active ingredients for suppressing ARD – whatever is inexpensive locally
Easy to manufacture with traditional equipment
Heat-seeking missile effect
Pumpable or flow-able
Biodegradable surfactants can double as bactericides
Permeates unsaturated zones of mine waste to deliver anti-ARD “cocktail” that could last for decades, maybe longer

## Slide 37: Thank You
jgusek@golder.com
or
ddunham@cellularconcretesolutions.com
Nihil simul inventum est et perfectum
Latin Proverb

## Slide 38: Thank You
Nothing is invented and perfected at the same time
jgusek@golder.com
or
ddunham@cellularconcretesolutions.com
Latin Proverb